- Properties of Wood

  - Two main types of wood

    - Hardwoods

      - Characterized by losing leaves in the fall

      - About 200 different types commonly used

      - Typically are harder and stronger

      - Better able to resist wear and dents or scratches

      - Oak, maple, walnut, ash

      - Often used to make furniture because of nice surface appearance

    - Softwoods

      - From evergreen trees that don’t lose their leaves

      - Pine, Douglas fir, cedar

      - Often weaker, but much cheaper since less demand for use in fine furniture

      - Used a lot for framing, pallets, and paper since the surface texture doesn’t matter in these applications

  - Tree Shapes

WoodTree Shapes

    - Typically either a pyramid or oval shaped

    - Modulus of elasticity increases with height while the Shear Modulus decreases with height

    - E and G both increase as you move from the center (pitch) to the bark

      - Wind loads cause the greatest stresses at the outside of the cross section near the bark

      - Wind causes the majority of the loads applied to trees

      - Typically wind speed increases as you get farther from the ground

  - Cell Structure

WoodCell Structure

    - Softwoods

      - Larger, more open cells

      - Water is transported by the cells

    - Hardwoods

      - Mainly small cells

      - A few large vessels that carry water

  - Wood Grain

WoodWood Grain

    - The grain you see in wood is formed in the direction of cell fiber growth

    - Six main types of grain found in wood

    - May find many different grain patterns in wood cut from the same tree

      - Grain type depends on proximity to limbs and how the board was cut from the tree

    - Depending on application you may want a different type of grain

      - Structural Strength

        - Straight grain typically the strongest

      - Woodworking

        - Other grain patterns may be desirable since more visually appealing

  - Saw Patterns

WoodSaw Patterns

    - The saw pattern used can affect the properties of the wood obtained from a log

      - The properties of wood are highly dependent on the orientation of the grain

      - Two pieces from the same log can have much different properties due to the way they have been cut

        - Remember that wood properties vary across the cross-section from the pith to the bark

        - Properties also vary with height so a long board may have length-wise property variation

    - Plainsawing

      - A few cuts are off a side then the log is rotated 90°

    - Quartersawing

      - Log is first cut into quarters

      - Then each quarter is successively cut on either flat side

    - Flitchsawing

      - All cuts are parallel to one another with no turning of the log

  - Grades of Lumber

WoodGrades of Lumber

    - Depends on number of defects in a given length and width

      - Four common grades for hardwoods

        - Firsts and Seconds

        - Select

        - #1 Common

        - #2 Common

      - Different grading system for softwoods

    - Defects

      - Bow

        - Warp on the face of the board from end to end

      - Cup

        - Warp on the face from side to side

      - Cup

        - Warp along edge line

      - Knots

        - Loose knots can fall out weakening the board

      - Splits

      - Twist

  - Property Comparison

WoodProperty Comparison

    - Depends on type of wood and grain pattern present

    - Direction of load relative to load is also important

- Lab Procedure

  - We will be performing three tests on wood

  - Plate-Connector Joint Test (ASTM D1761)

    - We will do this test working as an entire section

    - Attach a Simpson MP14 plate connector to two 1”x2”x6” pine boards placed end-to-end

    - Attach a Simpson MP24 plate connector to two 1”x3”x6” pine boards placed end-to-end

    - Apply load to both specimens using a cross-head speed of 0.035 in/min and a maximum displacement of 0.600 in

    - Stop the test once the load starts to decrease and record the maximum load from the computer

  - Dowel Bearing Test (ASTM 5764)

    - Each group should select a 2”x4” block with a half-hole in it.

      - Hole will be either transverse or axial

    - Load block in testing machine and place a ¾” bolt in the hole

    - Move the cross head until it nearly touches the bolt

      - Zero the load and the gage length

    - Apply load using a cross-head speed of 0.04 in/min

    - Stop the test when the displacement is 3/8” or the max. load has been reached

  - Fastener Withdrawal Test (ASTM D1761)

    - Each group should select a fastener to test and drive it 1” into a pine block

    - Load the block in the testing machine

      - Use supplied equipment to grab the fastener head

      - Clamp the block to the base using the C-clamps

    - Apply load to the fastener and find the maximum load required to withdraw the fastener

- Lab Report

  - Formal report worth 100 points

    - Remember to attach your initialed data sheet

  - Plate-Connector Test

    - Report the max. load for each plate

    - Calculate the load per tooth for each plate

    - Discuss why you would select one plate over the other and give an example of where you would use the selected plate

  - Dowel Bearing Test

    - Report the yield load or the maximum load

    - Calculate the bearing strength of the pine block

    - Discuss a situation where you could use the information from the test

  - Fastener Withdrawal Test

    - Report the maximum load required to withdraw the fastener

    - Compare your results to the reference values on the memo

    - Also compare your selected fastener to the strongest fastener in the reference table

    - Discuss the pros and cons of using nails vs. screws

Reference Values

| Fastener Description | Maximum Withdrawal Force (lb) |
| --- | --- |
| 6d bright common nail | 49 |
| 8d bright common nail | 65 |
| 10d bright common nail | 103 |
| 16d common nail | 125 |
| #8 x 1.75” wood screw | 457 |
| #10 x 1.75” wood screw | 483 |
| #12 x 1.75” wood screw | 555 |

- Presentation

  - Each group will fill in the following information and two groups will answer questions abut the lab

| Fastener Description | Maximum Withdrawal Force (lb) |
| --- | --- |

- No lab next week