Tension Testing

Lab Background

In this lab we will be performing tension tests.  Tension testing is very useful because it shows many important properties of the material tested.  Knowing these properties can be helpful when deciding what material to use.

Lab Procedure

Each group will perform a tension test on two different materials.  One test will be on an A36 steel specimen and the second test will be on a different material selected by the group.  The following steps should be completed in the lab:

- Select an A36 steel sample (large or small) and one other material to test.

- Measure the cross-sectional dimensions and length before testing.

- Answer the computer’s questions about your specimen.

- Load the specimen in the tension testing machine making sure to get a full bite in the grips.

- Attach the strain-gage extensometer to the specimen.  Do not drop the extensometer.  It is very fragile and expensive.

- Apply load to the specimen.

- The machine’s two heads will then move apart applying load to the specimen.  The machine will continue applying load until the specimen fractures.

- Remove the extensometer from the specimen and hang it safely on the machine frame.

- Remove the specimen from the machine and measure the final cross-sectional dimensions near the fracture surface and the final length after piecing the specimen back together.

After performing each tension test, a stress-strain diagram will be plotted on the computer monitor.  These diagrams and the calculated properties will be sent to your group’s members through e-mail.

Lab Report

The report for this lab should be a formal report which will be worth 100 points.  Be sure to attach a printed copy of the results e-mailed to you.  In your report, create a table showing the experimentally determined mechanical properties of both the A36 steel specimen and the other material selected by your group.  The following properties should be included in the table: modulus of elasticity, yield strength (or 0.2% offset yield strength), ultimate tensile strength, % elongation at fracture, % reduction in area, engineering stress at fracture, and true stress at fracture.  All of these values will be found by the computer.  The formulas used by the computer to calculate the properties are given in the Equations section at the end of this memo.  The equations are given in case you need to refer to them but no hand calculations are required for this lab.  I would also like for you to find reference values for A36 steel to compare your experimental values against using percent error.  You may not be able to find reference values for all of the A36 steel properties.  If no reference value can be found, list N/A where the value belongs in the table.

In the appropriate sections of your report, discuss how well your experimental results for A36 steel match the reference values.  Include reasons for any large differences.  Also, compare your second material to the A36 steel specimen based on the properties in your table.  Next, I would like for you to describe one application where steel would be better suited compared to the second material tested by your group.  Then, describe a different application where the second material would be preferable to the steel.  Be sure to support your suggestions using the properties in your table.  Finally, look at ASTM standard E8, which covers tension testing, and find three things that were not performed or were performed incorrectly when testing the A36 steel.  Report these errors and give suggestions for changes that could be made to correct them.

Presentation

Each group will come to the board and write your experimental values for the following properties:

| Material | Modulus of Elasticity (ksi) | 0.2% Offset Yield Strength (ksi) | Ultimate Tensile Strength (ksi) | % Elongation |
| --- | --- | --- | --- | --- |

Then two questions will be asked of random groups.

Equations

Engineering Stress:		True Stress:			Engineering Strain:

S=FA0		σ=FA			e=Lf−LL0

S= engineering stress, psi		σ = true stress, psi		e= engineering strain, in/in

F= load, lb		F= load, lb			Lf = final gauge length, in

A0= initial cross-			A= cross-sectional area	L0 = initial gauge length, in                                                                                                                            sectional area, in2	                              when load measured, in2

Modulus of Elasticity:		% Elongation:			% Reduction in Area:

E=ΔSΔe		% Elong=Lf−L0L0(100%)	%RA=Af−A0A0(100%)

E= modulus of elasticity, psi		Lf = final length, in		Af = final cross-sectional

ΔS= change in engineering 		L0 = initial length, in		        area, in2

stress, psi						A0 = initial cross-sectional

Δe= change in engineering						        area, in2

strain, in/in

% Error:

%Error=Exp. Value-Ref. ValueRef. Value100%