- Stress and Strain

  - By performing tension tests we will learn the relationship between stress and strain in the tested materials as load is applied

  - Stress and strain are important because they help us characterize materials

    - Each material has a unique stress-strain curve

  - Stress

    - Without stress we would have to perform tests on every cross-sectional area of interest to find the max. allowable load

    - By dividing by the area we remove it as a variable so we only need to test one cross-section for each specific material we’re interested in

  - Strain

    - Without using strain we would have to test several specimens that are the lengths we are interested in using

    - Strain removes the length of your specimen from consideration by dividing the change in length by the initial length

  - For a given material, failure occurs at the same stress and strain regardless of cross-section or length

- Tension Testing

  - A very good test to perform since several different material properties can be determined

    - Most people would expect that you would learn how much stress it takes to break the material but there are several other properties that can be found during tension testing

    - Properties

      - Modulus of Elasticity

        - Measures the stiffness of a material

      - Yield Strength

      - Ultimate Tensile Strength

      - % Elongation

      - % Reduction in Area

  - Tension Testing Sample Shapes

TensionASTM StandardsStandard Testing Shapes

    - Consists of portion with reduced dimensions

      - Can anyone think of a reason why we would want a portion with reduced dimensions?  Where would the highest stresses be?

      - Usually ground and polished to reduce surface imperfections

      - Used for standardized testing when high accuracy is desired

      - We will use round bars without any special shape for simplicity

- Lab Procedure

  - Each group will perform a tension test on two different materials

    - One of the tested materials must be an A36 steel sample

      - Can test either the large or small samples

    - Each group also will select a different material to perform a tension test on

  - Measure the dimensions of your specimen before testing

    - Need to measure the cross sectional dimensions

    - Also measure the initial length of your specimens

    - Record these on a sheet of paper so when it is your group’s turn you already have the measurements to enter on the computer

  - Tension Testing Machine

TensionAssignmentEquipment and Experimental Procedures

    - We will be using Instron Universal Testing Machines (UTM)

    - The specimens will be loaded in the grips of the machine

      - Be sure to get a full bite on your specimen in the grips

    - A strain-gage extensometer will be connected to record the strain on the specimen

    - Load will then be applied as the machine’s heads will then move apart

    - Load and deflection data will be automatically recorded by the computer

    - Output will be a stress-strain diagram for the test performed

    - Be sure to record the dimensions of the specimen after fracture

      - Measure the same cross-sectional dimensions after fracture

      - Also measure the final length after piecing the specimen back together

- Stress-Strain Diagrams

  - Define the following

    - Formulas

      - S=FAo			σ=FA

      - e=ΔLLo=Lf−LoLo		E=ΔSΔe

      - %Elong.=Lf−L0L0100%	     %RA=Af−AoAo100%

  - Draw the following on the board

  - Linear Portion of Curve

    - Elastic deformation

      - If load is removed, the material will return to its original shape and size

      - The slope of this portion of the curve is the modulus of elasticity of the material

        - This is what you found for the sample data sets from the Spreadsheet Lab when you did linear regression

  - Yield Point

    - The point where the stress-strain relationship stops following a linear curve and becomes nonlinear

    - Point that divides elastic and plastic deformation

      - Plastic deformation is permanent and remains even if the load is removed

    - Some materials have a better defined yield point than others

    - Steel should have a yield point that is easy to find

    - Other materials may not

  - 0.2% Offset Yield Point

    - Used when there is no clear yield point on the graph

    - Start a line at 0.002 in/in strain and use slope of initial portion of the stress-strain curve

    - Where line intersects the stress-strain curve is the 0.2% offset yield point

  - Plastic Portion of Curve

    - If load is removed, there will be permanent deformation from the original dimensions

    - Maximum point shows ultimate tensile strength

    - Necking begins at ultimate tensile strength

    - Once necked, less force is required to pull the specimen apart, so the engineering stress decreases

    - True stress continues to increase until fracture

  - Fracture

    - Final point on the graph is where the specimen has broken into two pieces

TensionSpecimen ImagesMacroscopic Fracture Theory

    - Ductile materials

      - Fail due to shear stresses

      - Steel usually has a 45° fracture surface for axial loads

      - May be a cup and cone fracture (steel)

      - Or a straight line fracture (aluminum)

    - Brittle materials

      - Fail due to normal stresses

      - Straight across fracture

      - Not much necking or sign of impending failure

  - Testing a high temperatures or at high strain rates can change the observed stress-strain curve for a given material

- Assignment

  - Formal report worth 100 points

    - Attach your computer print outs

    - Create a table of experimental mechanical properties for both materials tested

      - Modulus of Elasticity

      - Yield strength or 0.2% Offset yield strength

      - Ultimate Tensile Strength

      - Engineering Stress at Fracture

      - True Stress at Fracture

      - % Elongation

      - % Reduction in Area

    - Find reference values only for your A36 steel specimen

      - Compare your A36 experimental values to the reference values using percent error

        - %Error=Experimental−ReferenceReference100%

      - You may not be able to find reference values for all properties

        - If none, list N/A

    - Discuss reasons why your experimental values may be different from the reference values

    - Compare your second material to steel and show how the two differ

      - Describe one application where the second material would be preferable to steel and one application where the second material would not be as good as steel

    - Also look on Blackboard at ASTM standard E8 and find (3) things that were not performed or that were performed incorrectly when testing the A36 steel specimen

- Presentation

  - Each group will come to the board and write your experimental values for the following properties

| Material | Modulus of Elasticity (ksi) | Yield Strength (ksi) | Ultimate Tensile Strength (ksi) | % Elongation |
| --- | --- | --- | --- | --- |

  - Two questions will then be asked of random groups: