- Importance of Compression Testing

  - Compression testing gives properties similar to those found from our tension tests

  - Material behavior

    - Some materials behave nearly the same in compression as they do in tension

      - Ductile metals are a good example

    - Other materials behave much differently when subjected to compressive loads rather than tension loads

      - Brittle materials such as concrete or most ceramics

      - Very strong in compression when compared to tension

    - Complete Stress-Strain Diagram

      - Shows a material’s reaction to both tensile and compressive loads on one diagram

- Failure Methods for Compression Testing

  - During tension testing there was only one way for the material to fail

    - Necking and then pulled in to two halves

  - Compression tested material can fail in one of two ways

    - Excessive stress above the compressive yield strength or the compressive ultimate strength

      - Leads to yielding or the material cracking or breaking into two or more pieces

    - Buckling

      - Mainly happens for long narrow columns loaded in compression

      - Caused by the column deflecting away from being straight and becoming curved

      - Examples

CompressionIntroduction

        - Railroad tracks rigidly fixed together expanding on a hot day

        - Alaskan pipeline was laid out to avoid long straight sections that could buckle

      - Euler Buckling Formulas

        - Whether a column will fail due to buckling depends on whether the amount of load or stress applied is above a critical level

        - Critical load

        - Critical stress

        - Critical load and stress formulas are derived for a column with pin connections on both ends

        - If a different end connection is used then the effective length (Le) will be different

CompressionEuler Buckling

          - More rigidly the ends are held the harder it is to buckle the column

- Lab Procedure

  - Each group will perform one compression test on a wood block

    - You can either perform a compression test parallel to the grain or perpendicular to the grain

    - For a parallel to the grain test you will need to select a 2”x3”x8” block

    - For perpendicular to the grain testing you will need a 2”x3”x6” block

  - Parallel-to-grain test

    - Put marks 6” apart on your specimen that are centered from end to end

    - Attach a 6” mechanical extensometer to your specimen at the marks

    - Insert your specimen to the Instron 4485 testing machine

    - Set the cross-head speed to 0.024 in/min

    - Apply a compressive load to your block and record the deformation at each 1000 lb increment of load

    - Stop the test once a maximum load has been reached

  - Perpendicular-to-grain test

    - Insert your specimen to the Instron 4469 machine

    - You will use a dial gage to measure the deformation during the test

    - Set the cross-head speed to 0.012 in/min and record the load every 0.0025 in

    - Stop the test when a maximum load has been reached or the deformation is 0.1 inches, whichever occurs first

- Lab Report

  - Memo written by your group worth 100 points

  - Remember to attach your initialed data sheet

  - Create a stress-strain diagram using your data

  - Find the compressive modulus of elasticity by applying linear regression to a portion of the stress-strain curve that appears linear

    - Justify your selected area for regression

    - The slope of your regression line will be the compressive modulus of elasticity

  - Also find the compressive strength of your block by applying the following:

  - If you perform the parallel-to-grain test then you will also need to find the load at which your block would begin to buckle

    - Our end conditions would be considered fixed-free

    - The moment of inertia you should use is the minimum I for the cross-section

    - Use your experimentally determined E in your calculation

  - Comparisons to reference values

    - Compare your experimental compressive modulus of elasticity and compressive strength of your block to the reference values given on the data sheet

      - Use % error

      - Give reasons to justify your differences

  - Discuss in your memo a situation where it would be useful to know the compressive modulus of elasticity

  - Also discuss another real world application where it would be helpful to know the compressive strength of your block

- Presentation

  - Each group will come to the board and fill in the following information

| Load Direction | Comp. E (psi) | SUC (psi) | Pcr (lb) |
| --- | --- | --- | --- |

  - Then two groups will be selected answer questions about the lab