- What are fasteners and how are they used?

  - Fasteners literally include the nuts and bolts that hold everything together along with rivets, pins, nails, and other hardware used to hold two parts together

  - The types of fasteners we will test today include: bolts, washers, and nuts

- Classification of fasteners

  - There are two very common classification systems used for fasteners:

    - Society of Automotive Engineers (SAE)

IDE 120LessonsFastener TestingIntroduction

      - Classified by grades from 0-8

      - Higher grade numberStronger material used

      - General Rule

        - Count number of radial lines and add 2 to find the grade of the fastener

      - Grade 2

        - No markings on head other than manufacturer identification

        - Low carbon steel

        - Used for holding wood together or in applications where high strength is not required

      - Grade 5

        - 3 radial lines on head

        - Medium carbon steel with quench and temper HT

        - Used where moderate strength is required

      - Grade 8

        - 6 radial lines on head

        - Medium carbon alloy steel with quench and temper for high strength and hardness

        - Used when high strength is required

        - With higher strength comes less ductility

    - ASTM

      - Classified by letter and number

        - Usually stamped on head of bolt

        - Other identifying marks on nuts

        - Example is A 325

- Fastener terminology

Fastener TestingDefinitions

  - Threads

    - Major diameter

      - This dimension is what you see when buying fasteners

      - A ¼” bolt has a ¼” major diameter

    - Minor diameter

      - Measured after threads are cut

      - Smallest diameter of screw thread

    - Pitch

      - Tells the distance between identical locations on two threads

      - In English units, usually use reciprocal of pitch or threads per inch (tpi)

      - Metric uses pitch

    - Thread angle

      - Standardized at 60° for U.S. and Britain

    - Thread Designation Systems

      - American National (Unified) Thread Standard

        - Coarse Threads (UNC)

          - Fewer tpi than fine threads

        - Fine Threads (UNF)

          - More tpi than coarse

        - How to specify

          - Major diameter – tpi x Length

          - Example ¼”-20 x 1”

- Lab Procedure

  - Each group will perform hardness tests and a tension test on a 3/8”-16 bolt

    - Hardness Test

      - Should be done before tension test

      - According to Section 3.1

        - Test at locations for routine inspection

        - Follow the laboratory inspection procedure

      - Estimate tensile strength based on hardness value using same chart as was used for the hardness testing lab

    - Tension test

      - Perform according to Section 3.4

      - Gives an actual value for the tensile strength of the bolt

      - Make sure bolt fractures at a location specified in the standard

      - Calculate the actual tensile strength of the bolt using:

      - For the bolts tested: D=3/8” and N= 16 tpi

  - Each group will also need to perform hardness tests on one other fastener

    - You have your choice of a nut or washer for this second fastener

    - Make sure to draw your fastener and label the testing locations

    - Use ASTM Standard F606 to guide your testing procedure

      - F606 sometimes has more than one test location that can be used

      - Use the test location(s) for routine inspection if more than one is given

      - Make sure to read through the entire section that covers your fastener before beginning your test to avoid incorrectly testing your fastener

        - For hardness testing of nuts use Section 4.1

        - For hardness testing of washers use Sections 5.1-5.4

- Assignment

  - Complete provided data sheet which is worth 50 points and turn in before you leave today

- When finished with lab

  - If you are not taking the final you are free to leave after finishing the fastener testing lab

  - If you are taking the final please return to the classroom and we will begin the final once everyone has completed the lab