- Strain Gages

- What is a strain gage?

  - A piece of thin metal foil etched with parallel lines of foil left to measure strain

ElasticOptions

  - Attached to the part on which you wish to measure the strain

- Pros and Cons of Strain Gages

  - Pros

    - Very versatile and inexpensive

      - Many different sizes available

      - Many different materials for specific applications

    - Can be used on a curved surface

    - Very accurate if selected and used correctly

    - Can measure both static and dynamic loads

  - Cons

    - Once they are applied to a part, they cannot be removed without ruining the gage

    - Installation requires attention to detail to be performed correctly

    - Need a special instrument to measure the strain

- How a strain gage works

  - Strain is measured by measuring the change in the resistance of the foil “wires”

    - When the wires stretch or contract the length and cross-sectional areas change

    - A Wheatstone bridge circuit is used to measure the change in resistance for the strain gage

  - Gage Factor

    - Supplied by the manufacturer

    - GF=2.0 for most typical strain gages

    - R is the gage resistance and is typically 120 Ω

- Orientations of Strain Gages

ElasticOptions

  - Uniaxial Gages

    - Used when the principal direction is known or only interested in strain in a certain direction

    - Can only measure strain in the direction the wires are oriented

  - Biaxial Gage Rosettes

    - Two strain gages oriented perpendicular to one another

    - Used to measure both principal strains when the direction is known

  - Three Element Rosettes

    - Three gages oriented in a certain way

      - Example is 0, 45, and 90º

    - Allows you to measure the principal strains and determine the principal direction

- Real World Applications of Strain Gages

ElasticApplications

- Monitoring Structures

  - Used in bridges to measure the strains and stresses

  - Monitoring strain around a hole drilled to stop crack propagation

  - Why would you drill a hole at the tip of a crack?

- Design

  - Can be used to determine the stresses and strains in a complex geometry

- Three elastic constants studied in this lab

  - Called elastic constants because they only apply when the stress in the material is below the proportional limit where the material yields and becomes plastic

  - Modulus of Elasticity

    - Measures the stiffness of a material

    - Defined as the ratio of normal stress to the corresponding normal strain when below the proportional limit

  - Poisson’s Ratio

    - Defined as the ratio of transverse strain to axial strain caused by a uniform axial stress below the proportional limit

  - Modulus of Rigidity

    - Ratio of shear stress to the corresponding shear strain when below the proportional limit

- Reasons why elastic constants are important

  - These constants allow us to relate the stress and strain found in a part

    - Only have to measure either stress or strain and then can calculate the other

- Hooke’s Law

ElasticHooke’s Law

  - Mathematical relationship between stress and strain

    - Uses elastic constants that we will determine today

  - Form of equations depends on the type of material and the type of loading applied

    - In its most general form Hooke’s law requires the determination of 81 elastic constants

    - Also must solve 9 equations in 9 unknowns

  - Assumptions about materials for this lab

    - Linear

      - Linear relationship between load and deformation

    - Elastic

      - Stay in range where deformation is not permanent

      - Material returns to original shape and size if load is removed

    - Homogeneous

      - Material composition is the same throughout

    - Isotropic

      - Material properties are the same in all directions

      - Can anyone name a common material that would not be isotropic?

        - Wood and fiber reinforced materials

- Lab Procedure

  - Flexure Test

    - Draw picture of setup on the board

    - Make all necessary measurements

      - Length between supports

      - Cross-sectional dimensions of beam

      - Distance to the strain gages from the support

    - There are two strain gages on the beam

      - One measures strain in the axial direction

      - The other measures strain in the transverse direction

    - Put the weight hanger on the beam making sure it is centered between the supports and the hanger doesn’t touch anything other than the beam

    - Set up the strain indicators

      - Connect the wires from the strain gages

      - Zero the amp

      - Set the gage factor

      - Balance the strain

    - For the larger aluminum bar

      - Add weights in 5 lb increments until the total weight is 50 lb

      - Take readings of strain at every 5 lb increment and record on your data sheet

    - For the smaller aluminum bar or the magnesium bar

      - Add weights in 1 lb increments until the total weight is 10 lb

      - Take readings of strain at each 1 lb increment

    - Your group can decide which type of beam to test

      - Need to test two beams per group

  - Tension Test

    - The back of the data sheet is for tension test data

    - We will not be performing tension tests since we will use flexure tests instead

- Calculations

  - Flexure Test

    - Input your data to Excel and create two plots

      - Load vs. axial strain

      - Transverse strain vs. axial strain

    - Use linear regression to find the slope of a regression line for both plots

      - Plot your linear regression lines on the graphs and show the equations

    - Poisson’s Ratio

      - Slope from your transverse strain vs. axial strain graph

    - Modulus of Elasticity

      - (Go through derivation)

    - Modulus of Rigidity

      - Find this using values from flexure test by applying the following

- Assignment

  - Memo written by your group worth 100 points

    - Attach your group’s initialed data sheet

    - Include the graphs you need to create from your data

    - Show sample calculations

    - Summarize your calculated values in a table

  - Written part

    - Look up reference values for E, G, and Poisson’s ratio

    - Compare your calculated values to the reference values using percent difference

- Presentation

  - Each group will come to the board and write their experimental values for the following

| Material | E | G |  |
| --- | --- | --- | --- |