- Material Designation and Numbering Systems

  - Steel

    - Steel is composed mainly of iron and carbon with other elements added to create alloys

    - The AISI-SAE numbering system is very widely used

HardnessSteel Designation System

      - In this system a certain alloy is designated with a 4 digit number

      - The first two numbers specify the alloying elements

      - The last two numbers specify the carbon content of the steel in hundredths of a percent

  - Aluminum

    - AISI system is again widely used

HardnessAluminum Designation System

      - A 4 digit number is used for a wrought alloy

      - A 3 digit number is used for a casting alloy

      - The first digit tells what the major alloying elements are

    - Temper Designation

      - An additional letter and number attached to the end of the number

      - Tells how the material has been heat treated

- What is hardness testing and why is it important?

  - Hardness testing is not covered in IDE 110

  - Can someone give an everyday definition for hardness?

  - Hardness is defined as “The ability to  resist permanent indentation”

  - Hardness values alone tell us nothing unless we know what testing method was used

  - Advantages of hardness testing

    - Fast

    - Inexpensive

    - Nondestructive

      - If testing is performed properly using the correct method/indenter  for a given material

    - Can be done on a variety of materials if correct test is selected (Don’t want this to become destructive testing)

  - Use of material hardness information

    - Can be used to approximate the tensile strength of a material

    - Gives information about the material’s resistance to surface wear and abrasion

- Types of Hardness Tests

  - Most hardness tests involve indenting the surface of a material with an indenter

HardnessTechniques and EquipmentBrinell

    - Indenter shapes and materials

      - Ball, cone, pyramid

      - Hardened steel, diamond, carbide

    - Indenter size determines scale of the test

      - We will do macro scale hardness testing

  - A given load is applied for a prescribed amount of time using a specified indenter and then a measurement is made

  - Some testing machines require manual measurement of indention (Brinell)

  - Others will give a direct reading of hardness number from a gage (Rockwell)

  - Demonstrate some of the different testing devices on hand

- Lab Procedure

  - Each group member will perform the following tests

    - Brinell test on metal specimen

    - Rockwell test on metal specimen

    - Polymer hardness test

  - Only select materials that have a reference value given on the data sheet for the test you want to perform

  - Have a reason behind your selection of materials

- Brinell Test

  - We will perform the Brinell test using a 3000 kg load and a 10 mm hardened steel ball indenter

  - Commonly used on:

    - Cast iron

    - Steel

    - Smaller loads are used on softer materials when performing Brinell tests

  - Each person will perform one Brinell hardness test on a metal specimen

    - Select a location at least 2.5 times the indention diameter away from an edge of the specimen or the edge of an indention from a previous test

  - I will show you how to use the machine once we’re in the lab

  - After running the test you will measure the diameter of the indention using a microscope

    - Take two measurements 90° apart and average them

      - The reading you get from the microscope will be in mm

      - If indention is too large to read with microscope you will have to use calipers to measure the diameter

    - Use the chart on the machine (or formula) to find the Brinell Hardness number (HB)

      - Formula will likely be needed if you test  a copper specimen

      - Remember that the calipers measure in inches and the formula and chart use millimeters

  - Next you will estimate the tensile strength

    - Chart located on wall or ASTM E140 available on the IDE 120 website

      - Don’t need to interpolate unless you want to

- Rockwell B/C Test

  - The Rockwell B test uses a 1/16” diameter steel ball indenter

  - Rockwell C test uses a diamond cone indenter

  - Two loads are applied during the test

    - Minor load of 10 kg applied first

    - Major load of 100 kg applied after minor

  - Each person will do three Rockwell tests on your specimen

    - Distance between any two indentions should be 3 times the indention diameter

    - Center of all indentions must be at least 2.5 times the indention diameter away from the edge of the specimen

  - I will show the test method in the lab

    - The machine will give a direct reading for the Rockwell B/C hardness

    - Record the hardness as XX HRB on your data sheet

      - Find the average

    - If the HRB is above 100 you should use the HRC test

  - If using a cylindrical specimen you need to apply a correction factor to the value given by the machine

    - Correction factors can be found from the chart on the wall or Tables 11 and 12 in ASTM E18

  - Use the wall chart to estimate tensile strength based on the average Rockwell hardness

- Polymer Test

  - There are several choices of tests to perform on the polymers

  - First select a polymer and then perform a test that has a reference value given on the data sheet

    - Procedure to follow will vary depending on the test you perform

    - Will need to perform three tests on your specimen

    - Then average the three hardness values to find the hardness value you will report

    - Do not need to estimate tensile strength of the polymer you test

- Assignment

  - Formal report worth 100 points

    - Summarize what your group was trying to determine when selecting your materials

    - Create a table showing your results

      - Compare your hardness and tensile strength results with the reference values

        - Reference values are provided on the data sheet

        - Use % error

        - If a range of reference values is given, find the average and use as the reference value

        - There will be no % error comparison for the tensile strength of the polymer since you will not have an experimental value for it

        - Example of table

| Material | Exp. Hardness | Ref. Hardness | % Diff. Hardness | Exp. Tensile Strength (ksi) | Ref. Tensile Strength (ksi) | % Diff. Tensile Strength |
| --- | --- | --- | --- | --- | --- | --- |

        - Attach initialed data sheet from lab to memo

    - Discuss how well your experimental values match the reference values

      - Give reasons for any major differences

    - Describe one situation where you would rather use a Brinell hardness test and a different situation where you would prefer to use a Rockwell hardness test

- Presentation

    - Each group will come forward and fill in a table with the following for one of the metals tested by your group:

| Material | Hardness Test Performed | Avg. Hardness Value | Estimated Tensile Strength (ksi) |
| --- | --- | --- | --- |