- Torsion Testing

  - What is a torsion test?

    - Torsion tests apply a load to a specimen by twisting the ends of the specimen in opposite directions

  - Why perform a torsion test?

    - Get several values similar to those from a tension test

    - Values obtained include:

      - Modulus of Rigidity

        - Sometimes called the Shear Modulus

        - Similar	 to Modulus of Elasticity for tension test

      - Shearing Yield Point

      - Ultimate Shear Strength

      - Maximum Elastic Torque

      - Fully Plastic Torque

- Lab Procedure

  - We will split into two large groups to perform the tests

    - One large group will work with me on one machine

    - Other large group will work with TA on other machine

    - Each group needs to collect their own data

      - For Example: Group 1, 2, and 3 each have their own data sheet even though the data will be identical between groups

  - An A36 steel bar will be used in the tests

  - Equipment used

TorsionAssignmentTorsion Testing Equipment

  - Measurements

    - Diameter of the rod before testing

    - Troptometer radius

      - This needs to be from the center of the bar to the tip of the pointer

      - Easiest to find by measuring from the outside of the bar to the pointer and then adding on the radius of the bar

  - One end of the bar will remain fixed while the other end is slowly twisted by applying torque

    - You will collect data at each 100 in-lb increment of torque from 0 to 1000 in-lb of torque

    - Once the torque is above 1000 in-lb you will take readings at every 0.1 in  increment of arc length

      - Continue these readings until the fully plastic torque has been clearly reached

        - Fully plastic torque occurs when the bar continues to twist but the amount of torque required remains constant

      - It is up to the groups to decide when enough data points have been collected

        - Want several data points in the fully plastic region to ensure good results

    - After fully plastic torque has been established you will no longer need to collect data at regular intervals

      - We will continue to twist the bar until it fractures

      - Only thing left to find will be the maximum torque

- Torque vs. Angle of Twist Diagram

  - These are the values you will actually be recording in the lab

  - Show how to determine the Fully Plastic Torque and the Maximum Elastic Torque

  - Draw figure on board

Linear Elastic Portion

  - Formulas

    - (polar moment of inertia for circular cross section)

    - read from data and graph

- Shearing Stress-Strain Diagram

  - Element on the surface of the bar oriented along the axis

    - Has only shear stresses acting on it (pure shear)

    - Draw figure on board

  - Similar to tension stress-strain diagrams

    - Normal Stress is replaced by Shear Stress

    - Normal Strain is replace by Shear Strain

    - Assumes a linear elastic, perfectly plastic material

    - Draw figure on board

τy

G

  - Formulas

    - (applies only in linear elastic portion)

- Yielding in Circular Shafts

TorsionShort Version

  - Yielding starts at outer surface since maximum stresses are present there

  - As material yields there is a plastic shell that forms on the outside of the material

  - Eventually the entire cross section will yield and the fully plastic state will be reached

- Fracture Surfaces

  - Ductile Materials

    - Fail due to shear stress

    - Fracture surface should be oriented with shear stresses on element

    - Results in a 90º fracture surface

TorsionFracture Geometry

  - Brittle Materials

    - Fail due to normal stresses

    - Remember that an element oriented 45º from a pure shear element has only normal stresses

    - Results in brittle materials fracturing with a 45º fracture surface

  - The fracture surfaces are oriented just the opposite of what we found in the tension tests

- Direct Shear Test

  - While we are waiting on the torsion testing specimen to fracture we will perform a direct shear test

  - Will work as an entire section

  - Material to test will be an A36 bar identical to the one used for torsion testing

  - Procedure

    - Measure the diameter of the A36 steel bar

    - Load specimen in the shear testing fixture

    - Apply load to the specimen using a cross-head speed of 0.1 in/min

    - Run the test until the computer stops the cross-head

    - Record the 0.2% offset yield load from the computer

    - Record the maximum load from the computer

  - Calculations

    - Find the shearing yield strength by applying

    - Find the ultimate shearing strength using

- Assignment

  - Memo worth 100 points

    - Attach your initialed original data sheet

    - Experimental Results

      - Torsion Testing

        - Create a plot of torque (T) vs. angle of twist(φ) using your data

        - Based on your data and plot

          - Determine the Fully Plastic Torque (TFP)

          - Calculate the Maximum Elastic Torque (TE)

        - Use linear regression to calculate the slope of the linear elastic portion of the plot

          - Only use data points up to the Maximum Elastic Torque

        - Use your slope to calculate the modulus of rigidity (G)

        - Calculate the shearing yield strength and ultimate shearing strength

      - Direct Shear Testing

        - Calculate and report the shearing yield strength

        - Calculate and report the ultimate shearing strength

    - Discussion of Results

      - Discuss how well your data points fit the linear regression line

      - Compare your shearing yield strength and ultimate shearing strength between the torsion test and the direct shear test

      - Look up a reference value for G and compare your experimental value to the reference value

- Presentation

  - Each group will come to the board and fill in the following values

| TE (in-lb) | TFP (in-lb) | Experimental(ksi) | Experimental G (ksi) |
| --- | --- | --- | --- |

  - Two random groups will be selected to answer questions about the lab