Materials Testing Laboratory

Interdisciplinary Engineering Department

University of Missouri - Rolla

IDE 120 Flexure Test for Fully Plastic Action

File name: fully plastic action.is_flex

| Lab section | A |
| --- | --- |
| Group number or name | 1 |
| Temperature (F) | 75.0 |
| Humidity (%) | 29.0 |
| Fixture type | 3-point |
| Source for flexure strain | Extension |
| Email to | jthomas@umr.edu |

|  | Material Type | Diameter (in) | Support Span (in) | Crosshead Speed (in/min) |
| --- | --- | --- | --- | --- |
| 1 | A36 steel | 0.623 | 5.000 | 2.000 |
| 2 | A36 steel | 0.623 | 5.000 | 2.000 |
| 3 | A36 steel | 0.623 | 5.000 | 2.000 |
| Mean |  | 0.623 | 5.000 | 2.000 |

|  | Load at Cursor (lbf) | Extension at Cursor (in) | Maximum Load (lbf) | Extension at Maximum Load (in) |
| --- | --- | --- | --- | --- |
| 1 | 1668 | 0.091 | 2345 | 0.534 |
| 2 | 1669 | 0.082 | 2354 | 0.532 |
| 3 | 1682 | 0.089 | 2357 | 0.534 |
| Mean | 1673 | 0.087 | 2352 | 0.533 |

|  | Fully-Plastic Normal Stress (ksi) | Maximum Shear Stress (ksi) | Octahedral Shear Stress (ksi) |
| --- | --- | --- | --- |
| 1 | 51.74 | 25.87 | 24.39 |
| 2 | 51.76 | 25.88 | 24.40 |
| 3 | 52.17 | 26.09 | 24.60 |
| Mean | 51.89 | 25.95 | 24.46 |