Materials Testing Laboratory

Interdisciplinary Engineering Department

Missouri S&T

Tension Test with 1" Extensometer

File name: 1018 Rectangular.is_metal

| Number Inputs: Temperature (F) | 70.0 |
| --- | --- |
| Number Inputs: Humidity (%) | 50.0 |
| Data: Interval 1 | 0.10000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 100.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| General: Operator(s) | Jeff Thomas |
| Documents: Email to | jthomas@mst.edu |

Results

|  | Specimen Label | Geometry | Crosshead Speed (in/min) | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 |  | Rectangular | 1.000 | 33078 |
| 2 |  | Rectangular | 1.000 | 30011 |
| 3 |  | Rectangular | 1.000 | 34784 |
| 4 |  | Rectangular | 1.000 | 31478 |
| 5 |  | Rectangular | 1.000 | 32062 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 25204 | 0.464 | 101.6 | 0.50 |
| 2 | 24791 | 0.333 | 100.4 | 0.53 |
| 3 | 24966 | 0.451 | 100.5 | 0.48 |
| 4 | 24741 | 0.413 | 100.0 | 0.51 |
| 5 | 24912 | 0.374 | 100.9 | 0.51 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 25621 | 0.583 | 103.3 | 0.97 |
| 2 | 25471 | 0.491 | 103.1 | 2.37 |
| 3 | 25568 | 0.618 | 102.9 | 2.46 |
| 4 | 25428 | 0.595 | 102.7 | 2.72 |
| 5 | 25482 | 0.523 | 103.2 | 1.44 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 19887 | 0.838 | 80.2 | 1.12 |
| 2 | 19576 | 0.835 | 79.3 | 19.73 |
| 3 | 19651 | 0.928 | 79.1 | 22.81 |
| 4 | 19393 | 0.913 | 78.4 | 4.56 |
| 5 | 19630 | 0.821 | 79.5 | 1.91 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 7.2 | 20.6 | 0.348 | 0.998 |
| 2 | 7.4 | 381.0 | 0.358 | 18.509 |
| 3 | 7.0 | 443.8 | 0.336 | 21.431 |
| 4 | 7.2 | 92.8 | 0.348 | 4.500 |
| 5 | 7.2 | 37.1 | 0.350 | 1.800 |

|  | True Break Stress (ksi) | Reduction of Area (%) | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) |
| --- | --- | --- | --- | --- |
| 1 | 129.8 | 38.234 | 0.66 | 0.88 |
| 2 | 140.9 | 43.771 | 2.03 | 19.47 |
| 3 | 142.0 | 44.314 | 2.16 | 22.58 |
| 4 | 120.3 | 34.874 | 2.39 | 4.31 |
| 5 | 121.2 | 34.415 | 1.11 | 1.66 |

|  | Strength Coefficient, K (ksi) | Strain Hardening Exponent, n () | Break Location | Specimen note |
| --- | --- | --- | --- | --- |
| 1 | ----- | ----- | Outside GL |  |
| 2 | 115.6 | 0.024 | Inside GL |  |
| 3 | 115.0 | 0.023 | Inside GL |  |
| 4 | 115.2 | 0.024 | Outside GL |  |
| 5 | ----- | ----- | Outside GL |  |

Dimensions

|  | Intial length (in) | Initial width of plate (in) | Initial thickness of plate (in) | Initial diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 | 1.000 | 0.248 |  |
| 2 | 12.0000 | 0.996 | 0.248 |  |
| 3 | 12.0000 | 0.998 | 0.249 |  |
| 4 | 12.0000 | 0.998 | 0.248 |  |
| 5 | 12.0000 | 0.996 | 0.248 |  |

|  | Initial outer diameter of tube (in) | Initial wall thickness of tube (in) | Initial linear density (tex) | Initial area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.248 |
| 2 |  |  |  | 0.247 |
| 3 |  |  |  | 0.249 |
| 4 |  |  |  | 0.248 |
| 5 |  |  |  | 0.247 |

|  | Final length (in) | Final width of plate (in) | Final thickness of plate (in) | Final diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 | 0.828 | 0.185 |  |
| 2 | 12.0000 | 0.817 | 0.170 |  |
| 3 | 12.0000 | 0.814 | 0.170 |  |
| 4 | 12.0000 | 0.810 | 0.199 |  |
| 5 | 12.0000 | 0.810 | 0.200 |  |

|  | Final outer diameter of tube (in) | Final wall thickness of tube (in) | Final linear density (tex) | Final area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.153 |
| 2 |  |  |  | 0.139 |
| 3 |  |  |  | 0.138 |
| 4 |  |  |  | 0.161 |
| 5 |  |  |  | 0.162 |