Materials Testing Laboratory

Interdisciplinary Engineering Department

Missouri S&T

Tension Test with 1" Extensometer

File name: 1018 Small Cylindrical.is_metal

| Number Inputs: Temperature (F) | 70.0 |
| --- | --- |
| Number Inputs: Humidity (%) | 50.0 |
| Data: Interval 1 | 0.10000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 100.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| General: Operator(s) | Jeff Thomas |
| Documents: Email to | jthomas@mst.edu |

Results

|  | Specimen Label | Geometry | Crosshead Speed (in/min) | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 |  | Circular | 1.000 | 34998 |
| 2 |  | Circular | 1.000 | 32029 |
| 3 |  | Circular | 1.000 | 31510 |
| 4 |  | Circular | 1.000 | 31748 |
| 5 |  | Circular | 1.000 | 34136 |
| 6 |  | Circular | 1.000 | 32640 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 4392 | 0.093 | 90.9 | 0.45 |
| 2 | 4419 | 0.105 | 90.7 | 0.46 |
| 3 | 4473 | 0.110 | 91.9 | 0.50 |
| 4 | 4424 | 0.285 | 90.1 | 0.50 |
| 5 | 4367 | 0.119 | 89.7 | 0.49 |
| 6 | 4423 | 0.106 | 92.3 | 0.48 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 4942 | 0.436 | 102.3 | 4.49 |
| 2 | 4940 | 0.431 | 101.4 | 3.81 |
| 3 | 4953 | 0.378 | 101.7 | 3.16 |
| 4 | 4918 | 0.592 | 100.2 | 3.53 |
| 5 | 4856 | 0.453 | 99.7 | 3.97 |
| 6 | 4918 | 0.400 | 102.6 | 3.65 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 2993 | 0.664 | 62.0 | 10.74 |
| 2 | 3144 | 0.675 | 64.6 | 4.52 |
| 3 | 3103 | 0.583 | 63.7 | 3.51 |
| 4 | 3188 | 0.789 | 64.9 | 3.97 |
| 5 | 3024 | 0.723 | 62.1 | 5.02 |
| 6 | 3072 | 0.658 | 64.1 | 4.61 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 1.2 | 41.1 | 0.288 | 10.213 |
| 2 | 1.2 | 17.7 | 0.302 | 4.367 |
| 3 | 1.3 | 13.5 | 0.313 | 3.336 |
| 4 | 1.2 | 15.3 | 0.302 | 3.729 |
| 5 | 1.2 | 19.3 | 0.293 | 4.758 |
| 6 | 1.2 | 18.0 | 0.306 | 4.495 |

|  | True Break Stress (ksi) | Reduction of Area (%) | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) |
| --- | --- | --- | --- | --- |
| 1 | 178.8 | 65.342 | 4.20 | 10.57 |
| 2 | 185.2 | 65.147 | 3.50 | 4.32 |
| 3 | 185.4 | 65.620 | 2.83 | 3.31 |
| 4 | 182.8 | 64.478 | 3.21 | 3.76 |
| 5 | 183.1 | 66.089 | 3.68 | 4.84 |
| 6 | 173.9 | 63.120 | 3.34 | 4.41 |

|  | Strength Coefficient, K (ksi) | Strain Hardening Exponent, n () | Break Location | Specimen note |
| --- | --- | --- | --- | --- |
| 1 | 131.5 | 0.065 | Unsure |  |
| 2 | ----- | ----- | Outside GL |  |
| 3 | ----- | ----- | Outside GL |  |
| 4 | ----- | ----- | Outside GL |  |
| 5 | ----- | ----- | Outside GL |  |
| 6 | 131.1 | 0.062 | Outside GL |  |

Dimensions

|  | Intial length (in) | Initial width of plate (in) | Initial thickness of plate (in) | Initial diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.248 |
| 2 | 12.0000 |  |  | 0.249 |
| 3 | 12.0000 |  |  | 0.249 |
| 4 | 12.0000 |  |  | 0.250 |
| 5 | 12.0000 |  |  | 0.249 |
| 6 | 12.0000 |  |  | 0.247 |

|  | Initial outer diameter of tube (in) | Initial wall thickness of tube (in) | Initial linear density (tex) | Initial area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.048 |
| 2 |  |  |  | 0.049 |
| 3 |  |  |  | 0.049 |
| 4 |  |  |  | 0.049 |
| 5 |  |  |  | 0.049 |
| 6 |  |  |  | 0.048 |

|  | Final length (in) | Final width of plate (in) | Final thickness of plate (in) | Final diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.146 |
| 2 | 12.0000 |  |  | 0.147 |
| 3 | 12.0000 |  |  | 0.146 |
| 4 | 12.0000 |  |  | 0.149 |
| 5 | 12.0000 |  |  | 0.145 |
| 6 | 12.0000 |  |  | 0.150 |

|  | Final outer diameter of tube (in) | Final wall thickness of tube (in) | Final linear density (tex) | Final area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.017 |
| 2 |  |  |  | 0.017 |
| 3 |  |  |  | 0.017 |
| 4 |  |  |  | 0.017 |
| 5 |  |  |  | 0.017 |
| 6 |  |  |  | 0.018 |