Materials Testing Laboratory

Interdisciplinary Engineering Department

Missouri S&T

Tension Test with 1" Extensometer

File name: 4130 Cylindrical.is_metal

| Number Inputs: Temperature (F) | 70.0 |
| --- | --- |
| Number Inputs: Humidity (%) | 50.0 |
| Data: Interval 1 | 0.10000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 100.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| General: Operator(s) | Jeff Thomas |
| Documents: Email to | jthomas@mst.edu |

Results

|  | Specimen Label | Geometry | Crosshead Speed (in/min) | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 |  | Circular | 1.000 | 21990 |
| 2 |  | Circular | 1.000 | 20766 |
| 3 |  | Circular | 1.000 | 21010 |
| 4 |  | Circular | 1.000 | 20523 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 22076 | 0.189 | 72.9 | 0.50 |
| 2 | 21818 | 0.187 | 72.3 | 0.51 |
| 3 | 21799 | 0.192 | 72.2 | 0.51 |
| 4 | 21754 | 0.189 | 72.1 | 0.51 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 29466 | 0.787 | 97.3 | 7.17 |
| 2 | 29691 | 0.790 | 98.3 | 6.90 |
| 3 | 29444 | 0.791 | 97.5 | 7.26 |
| 4 | 29380 | 0.780 | 97.3 | 7.28 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 24601 | 1.307 | 81.2 | 20.87 |
| 2 | 26395 | 1.195 | 87.4 | 10.38 |
| 3 | 24956 | 1.310 | 82.7 | 28.27 |
| 4 | 23485 | 1.303 | 77.8 | 31.70 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 6.3 | 488.7 | 0.251 | 19.361 |
| 2 | 6.4 | 242.9 | 0.255 | 9.654 |
| 3 | 6.4 | 658.7 | 0.253 | 26.181 |
| 4 | 6.4 | 729.8 | 0.255 | 29.006 |

|  | True Break Stress (ksi) | Reduction of Area (%) | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) |
| --- | --- | --- | --- | --- |
| 1 | 130.5 | 37.740 | 6.73 | 20.50 |
| 2 | 115.7 | 24.422 | 6.43 | 9.96 |
| 3 | 127.1 | 34.964 | 6.79 | 27.87 |
| 4 | 128.7 | 39.562 | 6.80 | 31.33 |

|  | Strength Coefficient, K (ksi) | Strain Hardening Exponent, n () | Break Location | Specimen note |
| --- | --- | --- | --- | --- |
| 1 | 145.2 | 0.118 | Unsure |  |
| 2 | 150.1 | 0.126 | Outside GL |  |
| 3 | 147.3 | 0.123 | Unsure |  |
| 4 | 147.1 | 0.123 | Unsure |  |

Dimensions

|  | Intial length (in) | Initial width of plate (in) | Initial thickness of plate (in) | Initial diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.621 |
| 2 | 12.0000 |  |  | 0.620 |
| 3 | 12.0000 |  |  | 0.620 |
| 4 | 12.0000 |  |  | 0.620 |

|  | Initial outer diameter of tube (in) | Initial wall thickness of tube (in) | Initial linear density (tex) | Initial area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.303 |
| 2 |  |  |  | 0.302 |
| 3 |  |  |  | 0.302 |
| 4 |  |  |  | 0.302 |

|  | Final length (in) | Final width of plate (in) | Final thickness of plate (in) | Final diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.490 |
| 2 | 12.0000 |  |  | 0.539 |
| 3 | 12.0000 |  |  | 0.500 |
| 4 | 12.0000 |  |  | 0.482 |

|  | Final outer diameter of tube (in) | Final wall thickness of tube (in) | Final linear density (tex) | Final area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.189 |
| 2 |  |  |  | 0.228 |
| 3 |  |  |  | 0.196 |
| 4 |  |  |  | 0.182 |