Materials Testing Laboratory

Interdisciplinary Engineering Department

Missouri S&T

Tension Test with 1" Extensometer

File name: 1018 Cylindrical.is_metal

| Number Inputs: Temperature (F) | 70.0 |
| --- | --- |
| Number Inputs: Humidity (%) | 50.0 |
| Data: Interval 1 | 0.10000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 100.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| General: Operator(s) | Jeff Thomas |
| Documents: Email to | jthomas@mst.edu |

Results

|  | Specimen Label | Geometry | Crosshead Speed (in/min) | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 |  | Circular | 1.000 | 33547 |
| 2 |  | Circular | 1.000 | 35105 |
| 3 |  | Circular | 1.000 | 34994 |
| 4 |  | Circular | 1.000 | 32776 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 24613 | 0.190 | 81.0 | 0.44 |
| 2 | 24796 | 0.214 | 81.1 | 0.43 |
| 3 | 25082 | 0.194 | 82.5 | 0.43 |
| 4 | 24685 | 0.187 | 81.0 | 0.44 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 27834 | 0.571 | 91.6 | 5.82 |
| 2 | 27962 | 0.649 | 91.4 | 5.35 |
| 3 | 28467 | 0.615 | 93.7 | 5.85 |
| 4 | 28102 | 0.575 | 92.2 | 5.54 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 19458 | 0.956 | 64.0 | 8.10 |
| 2 | 19544 | 1.125 | 63.9 | 7.17 |
| 3 | 19479 | 1.160 | 64.1 | 19.32 |
| 4 | 19383 | 0.990 | 63.6 | 7.00 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 6.5 | 180.4 | 0.255 | 7.126 |
| 2 | 6.4 | 159.9 | 0.251 | 6.275 |
| 3 | 6.5 | 430.6 | 0.258 | 17.007 |
| 4 | 6.5 | 156.4 | 0.257 | 6.156 |

|  | True Break Stress (ksi) | Reduction of Area (%) | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) |
| --- | --- | --- | --- | --- |
| 1 | 146.7 | 56.338 | 5.54 | 7.91 |
| 2 | 151.7 | 57.875 | 5.09 | 6.99 |
| 3 | 155.0 | 58.644 | 5.59 | 19.13 |
| 4 | 154.2 | 58.777 | 5.25 | 6.81 |

|  | Strength Coefficient, K (ksi) | Strain Hardening Exponent, n () | Break Location | Specimen note |
| --- | --- | --- | --- | --- |
| 1 | ----- | ----- | Outside GL |  |
| 2 | ----- | ----- | Outside GL |  |
| 3 | 123.3 | 0.076 | Unsure |  |
| 4 | ----- | ----- | Outside GL |  |

Dimensions

|  | Intial length (in) | Initial width of plate (in) | Initial thickness of plate (in) | Initial diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.622 |
| 2 | 12.0000 |  |  | 0.624 |
| 3 | 12.0000 |  |  | 0.622 |
| 4 | 12.0000 |  |  | 0.623 |

|  | Initial outer diameter of tube (in) | Initial wall thickness of tube (in) | Initial linear density (tex) | Initial area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.304 |
| 2 |  |  |  | 0.306 |
| 3 |  |  |  | 0.304 |
| 4 |  |  |  | 0.305 |

|  | Final length (in) | Final width of plate (in) | Final thickness of plate (in) | Final diameter of cylinder (in) |
| --- | --- | --- | --- | --- |
| 1 | 12.0000 |  |  | 0.411 |
| 2 | 12.0000 |  |  | 0.405 |
| 3 | 12.0000 |  |  | 0.400 |
| 4 | 12.0000 |  |  | 0.400 |

|  | Final outer diameter of tube (in) | Final wall thickness of tube (in) | Final linear density (tex) | Final area (in^2) |
| --- | --- | --- | --- | --- |
| 1 |  |  |  | 0.133 |
| 2 |  |  |  | 0.129 |
| 3 |  |  |  | 0.126 |
| 4 |  |  |  | 0.126 |