Materials Testing Laboratory

Interdisciplinary Engineering Department

University of Missouri - Rolla

BE 120 Rectangular Tension Test with 1" Extensometer

File name: 4-6-05 4130 rect tension_11.is_metal

| Text Inputs: Section Letter | A |
| --- | --- |
| Text Inputs: Group Number or Name | 1 |
| Number Inputs: Temperature (F) | 78.0 |
| Number Inputs: Humidity (%) | 31.0 |
| General: System of units | US Customary |
| Data: Interval 1 | 0.05000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 95.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| Documents: Email to | jthomas@umr.edu |

|  | Material Type | Crosshead Speed (in/min) | Break Location | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 4130 steel | 1.000 | Outside GL | 33099 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 13781 | 0.173 | 89.6 | 0.48 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 16999 | 0.883 | 110.5 | 6.97 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 14819 | 1.198 | 96.3 | 8.51 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 3.8 | 112.3 | 0.299 | 8.760 |

|  | Initial Width (in) | Initial Thickness (in) | Initial Length (in) | Initial Cross-Sect. Area (in^2) |
| --- | --- | --- | --- | --- |
| 1 | 0.623 | 0.247 | 12.0000 | 0.154 |

|  | Final Width (in) | Final Thickness (in) | Final length (in) | Final Cross-Sect. Area (in^2) |
| --- | --- | --- | --- | --- |
| 1 | 0.513 | 0.184 | 13.0625 | 0.094 |

|  | Reduction of Area (%) | True Break Stress (ksi) | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) |
| --- | --- | --- | --- | --- |
| 1 | 38.659 | 157.0 | 6.63 | 8.22 |

|  | Strain Hardening Exponent at n-Value (Automatic) | Strength Coefficient at n-Value (Automatic) (ksi) |
| --- | --- | --- |
| 1 | ----- | ----- |