Materials Testing Laboratory

Interdisciplinary Engineering Department

University of Missouri - Rolla

BE 120 Cylindrical Tension Test with 1" Extensometer

File name: 4-12-05 a36 tension_2.is_metal

| Text Inputs: Section Letter | A |
| --- | --- |
| Text Inputs: Group Number or Name | 1 |
| Number Inputs: Temperature (F) | 76.0 |
| Number Inputs: Humidity (%) | 38.0 |
| General: System of units | US Customary |
| Data: Interval 1 | 0.10000 sec |
| Strain: Source for tensile strain | Strain 1 |
| Strain: Gauge width 1 | 1.00000 |
| Strain: Auto balance | True |
| Extensometer Removal: Value | 95.00000 % |
| End of Test: Sensitivity (%) | 20.00000 |
| Documents: Email to | jthomas@umr.edu |

|  | Material Type | Crosshead Speed (in/min) | Break Location | Modulus of Elasticity (ksi) |
| --- | --- | --- | --- | --- |
| 1 | A36 steel | 2.500 | Outside GL | 35583 |

|  | Load at 0.2%-Offset Yield (lbf) | Extension at 0.2%-Offset Yield (in) | Stress at 0.2%-Offset Yield (ksi) | Strain at 0.2%-Offset Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | 14936 | 0.354 | 48.7 | 0.33 |

|  | Load at Max. Load (lbf) | Extension at Max. Load (in) | Stress at Max. Load (ksi) | Strain at Max. Load (%) |
| --- | --- | --- | --- | --- |
| 1 | 20768 | 2.093 | 67.7 | 17.39 |

|  | Load at Break (lbf) | Extension at Break (in) | Stress at Break (Engineering) (ksi) | Strain at Break (%) |
| --- | --- | --- | --- | --- |
| 1 | 14352 | 3.062 | 46.8 | 28.19 |

|  | Yield Energy (ft-lbf) | Break Energy (ft-lbf) | Modulus of Resilience (ksi) | Modulus of Toughness (ksi) |
| --- | --- | --- | --- | --- |
| 1 | 3.3 | 458.5 | 0.130 | 17.934 |

|  | True Break Stress (ksi) | Initial Diameter (in) | Initial Length (in) | Initial Cross-Sect. Area (in^2) |
| --- | --- | --- | --- | --- |
| 1 | 140.2 | 0.625 | 12.0000 | 0.307 |

|  | Reduction of Area (%) | Final diameter (in) | Final length (in) | Final Cross-Sect. Area (in^2) |
| --- | --- | --- | --- | --- |
| 1 | 66.638 | 0.361 | 14.5000 | 0.102 |

|  | Elongation at Max. Load, Plastic (%) | Elongation at Break, Plastic (%) | Strength Coefficient at n-Value (Automatic) (ksi) | Strain Hardening Exponent at n-Value (Automatic) () |
| --- | --- | --- | --- | --- |
| 1 | 17.20 | 28.06 | 118.43124 | 0.21391 |